## Slide 1: SMD Compatible Ku-Band LTCC Circulators
N. Parker1, C. Kärnfelt2, R. Lebourgeois3, L. Roussel4, V. Laur1
1Université de Bretagne Occidentale, Lab-STICC, UMR CNRS 6285, Brest
2IMT Atlantique, Lab-STICC, UMR CNRS 6285, Brest
3Thales Research & Technology, Palaiseau
4Thales Land & Air Systems, Élancourt

## Slide 2: Outline
Background & Motivations
Manufacturing Technology
Circulator Design
Manufacturing & Soldering
Measurements
Conclusion

## Slide 3: Background & Motivations
Circulator
  3-port device
  Non-reciprocal
Common uses
  Amplification stage decoupling
  Full duplex system

## Slide 4: Background & Motivations
Switch from mechanically steered antenna to AESA
  ⇒ Requires a great number of Tx/Rx modules
Circulator drawbacks
  Expensive
  Bulky
  Hard to integrate

## Slide 5: Manufacturing Technology
LTCC Technology ?
  Low Temperature Cofired Ceramics (< 950 °C)
High flexibility
  2.5D Technology
  Multi-materials
  Easy to industrialize
Few ferrites available

## Slide 6: Manufacturing Technology
Development of new ferrite materials
  Garnet ferrite
    Moderate magnetization of 1900 G
    High relative permittivity of 21
  Spinel ferrite
    Increased magnetization of 3800 G
    Moderate relative permittivity of 13

## Slide 7: Circulator Design
LTCC Technology manufacturing
SMD compatible
7×7×0,352 mm
Ø3×2 mm magnet

## Slide 8: Circulator Design – Methodology & Materials
Nom | εr | tan δ | 4πMs (G) | ΔH (Oe)
Garnet | 21 | 3.10-3 | 1900 | 100 @ 10 GHz
Spinel | 13 | 1.10-3 | 3800 | 100 @ 10 GHz
VLF220Aq4 | 21 | 3.10-3 | - | -
Teflon™ | 2,1 | 1.10-3 | - | -
Nom | Br (KG) | Hcb (KOe)
Magsy YXG-28 | 10,3 - 10,8 | 9,5 - 10,2
Materials properties
Magnet properties
Design steps
  Y-Junction circulator sizing
  SMD transition design
  Complete SMD circulator simulation

## Slide 9: Circulator Design – Simulation setup
EM Ansys HFSS™ linked to the Magnetostatic solver Ansys Maxwell3D™
Internal magnetic field inhomogeneity is taken into account in the HFSS simulation
Maxwell3D™ Simulation
Calculation of the internal static field in the ferrite
HFSS™ Simulation
Calculation of the EM field propagation
Import of the static magnetic field map into HFSS
Calculation of the Polder tensors as a function of the local field strength

## Slide 10: Circulator Design – Y-junction Circulator sizing
Initial sizing done using Bosma’s model
Optimization of the dimensions using HFSS™
Design | Rf (µm) | la (µm) | wa (µm) | w50 (µm)
Garnet design | 1100 | 820 | 287 | 115
Spinel design | 1100 | 780 | 407 | 115

## Slide 11: Circulator Design – SMD transition design
Conventional SMD transition

## Slide 12: Circulator Design – SMD transition design
SMD transition modified for LTCC

## Slide 13: Circulator Design – Complete SMD circulator
Garnet circulator
Spinel circulator
13.5%
-0.51dB @16.22GHz
18.7%
-0.47dB @16.29GHz

## Slide 14: Manufacturing
Stacking
Tape cutting
Multi-layer stack
Backside screen printing
Topside screen printing
Circulator view before firing
Multi-circulator matrix manufacturing

## Slide 15: Soldering
Soldering on a Rogers substrate stack
PCB Design
Manufactured PCB
Soldered circulator on the connectorized PCB
X-Ray observation of the soldering

## Slide 16: Measurements – Setup
3-port measurements
Southwest connectors
Custom TRL calibration kit

## Slide 17: Measurements – Garnet circulator
15.3%
-0.48dB @14.48GHz
Notes: Pertes max à -18 dB 0.8db

## Slide 18: Measurements – Spinel circulator
32%
-0.47dB @15.88GHz
Notes: Pertes max à -18 dB 0.73db

## Slide 19: Conclusion
Both circulator achieved good performances
Validation of the SMD capabilities through successful soldering
Spinel ferrite more promising

## Slide 20: Références
[1] R. van Dijk, G. van der Bent, M. Ashari and M. McKay, "Circulator integrated in low temperature co-fired ceramics technology," 2014 44th European Microwave Conference, 2014, pp. 1544-1547, doi: 10.1109/EuMC.2014.6986744.
[2] Jensen, T., Krozer, V., & Kjærgaard, C. (2011). Realisation of microstrip junction circulator using LTCC technology. Electronics Letters, 47(2), 111. doi:10.1049/el.2010.2419
[3] L. Qassym, V. Laur, R. Lebourgcois and P. Queffelec, "Ferrimagnetic garnets for Low Temperature Co-fired Ceramics microwave circulators," 2018 IEEE/MTT-S International Microwave Symposium - IMS, 2018, pp. 750-752, doi: 10.1109/MWSYM.2018.8439250.
[4] P. R. Raj, A. Basu and S. K. Koul, "Comparison of triangular geometries of Y-junction in co-sintered LTCC based microstrip circulator," 2017 IEEE MTT-S International Microwave Workshop Series on Advanced Materials and Processes for RF and THz Applications (IMWS-AMP), 2017, pp. 1-3, doi: 10.1109/IMWS-AMP.2017.8247361.
[5] S. Yang, W. Shi, H. Bai and T. Zhang, "Circulator Integrated in LTCC with Screen Printed Co-Firing Ferrite for Space Application," 2018 International Conference on Microwave and Millimeter Wave Technology (ICMMT), 2018, pp. 1-3, doi: 10.1109/ICMMT.2018.8563702.

## Slide 21: Thank you for your attention! What are your questions?