## Slide 1: Towards W-band self-biased circulators for next generation of VHTS payload
E. Roue1-2, A. Chevalier1, G. Tanné1, R. Lebourgeois3, O. Vendier4, R. Jaoui5, V. Laur1
1Lab-STICC, University of Brest
2CNES
3Thales Research & Technology
4Thales Alenia Space
5DGA

## Slide 2: Outline
Context
Self-biased circulators principle
W-band rectangular waveguide circulator
W-band planar isolator
Conclusions and prospects

## Slide 3: Outline
Context
Self-biased circulators principle
W-band rectangular waveguide circulator
W-band planar isolator
Conclusions and prospects

## Slide 4: Context

## Slide 5: Context

## Slide 6: Outline
Context
Self-biased circulators principle
W-band rectangular waveguide circulator
W-band planar isolator
Conclusions and prospects

## Slide 7: Self-biased circulator principle
Ferrite
Dielectric
Microstrip Y-junction
Magnet
Standard circulator
Self-biased circulator
Soft ferrite
Magnetization state: saturation
Need a permanent magnet
Pre-oriented hexaferrite
Magnetization state: remanence
No permanent magnet
Easier integration
Permanent magnet
Hysteresis cycle of a soft ferrite
Hysteresis cycle of a pre-oriented hexaferrite
Happ
Happ

## Slide 8: Outline
Context
Self-biased circulators principle
W-band rectangular waveguide circulator
W-band planar isolator
Conclusions and prospects

## Slide 9: W-band rectangular waveguide circulator
Selection of a pre-oriented strontium hexaferrite
Previous successfull demonstration in Ku, Ka and Q band
  Laur et al. IEEE TMTT 2015
  Noutehou et al. SPCD 2018
  Parker et al. IEEE TMAG 2021
  Parker et al. IMS 2023
  Roué et al. EuMW 2023
Material |  |  |  |  |  | 
SrM | 21.3 | 5.10-4 | 4080 | > 0.85 | 17.5 | 200 @ 45 GHz
Material |  |  |  |  |  | 
SrM | 21.3 | 5.10-4 | 4080 | > 0.85 | 17.5 | 200 @ 45 GHz

## Slide 10: W-band rectangular waveguide circulator
Design and simulation:
Y junction circulator in WR-12 waveguide (60-90 GHz) with quarter-wavelength lines
Ferrite disk dimensions: Rf = 0.42 mm, hf = 0.6 mm
Preliminary design (Linkhart formulas) and Ansys HFSS optimization
In simulation: IL < 0.3 dB and Isolation > 20 dB from 71-76 GHz

## Slide 11: W-band rectangular waveguide circulator
Fabrication and measurements:
Component housing made of two blocks
Machined in aluminum with a silver coating (t > 5 µm)
Ferrite disk manually stuck at the center of the Y-junction
Fairly good agreement between simulation and measurement (slight shift toward low frequencies)
  ILmin = 0.37 dB at 71.6 GHz
  IL < 1.45 dB and Isolation > 14.8 dB between 71 and 76 GHz

## Slide 12: Outline
Context
Self-biased circulators principle
W-band rectangular waveguide circulator
W-band planar isolator
Conclusions and prospects

## Slide 13: W-band planar isolator
Isolator design due to measurement limitation (2 ports measurements only)  Circulator + 50Ω load
Y-junction in microstrip technology with quarter wavelength impedance transformers
Integration of coplanar-to-microstrip transitions (measurements using a probe station)
50Ω load: Ta2N resistive layer
1.2 mm
1.2 mm
71-76 GHz:
IL < 2.22 dB
Iso >13.5 dB
RL > 23.7 dB

## Slide 14: W-band planar isolator
Fabrication: machining and polishing, standard thin film process
Measurement: ZVA-67 with ZVA-110 frequency converters, Microtest probe station
Quite good agreement between measurement and simulation but slight shift toward low frequencies
IL < 2.29 dB and Isolation > 10.9 dB in the 71-76 GHz frequency band

## Slide 15: Outline
Context
Self-biased circulators principle
W-band rectangular waveguide circulator
W-band planar isolator
Conclusions and prospects

## Slide 16: Conclusion and prospects
Experimental demonstration of W-band self-biased circulators and isolators with state-of-the-art performance
  Rectangular waveguide  Comùpetitive with standard technology (spinel ferrites with permanent magnet)
  Microstrip  Promising results / Requires better control of design and process
Chart: RWG technology
| 73.5 | 34.5 | 30.25 | 96 | 32.799999999999997 | 96 | 91 | 41.4 | 43.2 | 41 | 42.9 | 39 | 71.599999999999994 | 73.5
Sous champ | #N/A | 0.1 | 0.1 | 0.5 | #N/A | 0.15 | 1.2 | #N/A | 1.23 | #N/A | 0.21 | #N/A
A la rémanence | 1.1 | #N/A | #N/A | #N/A | 1.5 | #N/A | #N/A | 1.79 | #N/A | 0.87 | #N/A | 0.41
Ce travail | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.37 | 0.89
Chart: Planar technology
| 94 | 94 | 94 | 94 | 32.5 | 32.5 | 34 | 28.9 | 29 | 41 | 38 | 58 | 28.7 | 38.1 | 37 | 36 | 38 | 38 | 37.200000000000003 | 35 | 60 | 60 | 71 | 82.5
Sous champ | #N/A | #N/A | #N/A | #N/A | 0.75 | #N/A | 5 | #N/A | 1.6 | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A
A la rémanence | #N/A | #N/A | #N/A | #N/A | #N/A | 4 | #N/A | 2.8 | #N/A | 3 | 6.9 | 8 | #N/A | 1 | 0.48 | 0.48 | 0.7 | 0.5 | 0.76 | 0.76 | 1.3 | 2.5 | #N/A | #N/A
Ce travail | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 1.77 | #N/A
w/ H field
w/o H field
This work
w/ H field
w/o H field
This work

## Slide 17: Towards W-band self-biased circulators for next generation of VHTS payload
E. Roué
Thank you for your attention