## Slide 1
SOLID STATE POLYMER MULTILAYER CAPACITORS
FOR HIGH TEMPERATURE APPLICATIONS
Angelo Yializis, Paul Roop and Akilavasan Jeganathan
Polycharge America Inc.
Tucson 85737,
Arizona, USA
ayializis@polycharge.com

## Slide 2
CAPACITORS OPERATING AT HIGH TEMPERATURE
Limited To High Temperature Applications That Require:
Stable Capacitance with Temperature and Bias
High Capacitance
High Voltage and
High Energy Density
Capacitor Technologies That Satisfy the Above Requirements
High Capacitance + Stable Capacitance with Temperature and Bias : Eliminates NPO and Ferroelectric MLCCs
High Voltage: Eliminates Ta Electrolytics
High Capacitance: Eliminates Mica and other Similar Dielectrics
This leaves Polymer Film Capacitors in Various Configurations - Metallized, Film Foil, Double Metallized Film Electrodes, Hybrids, and Metallized Paper
  If High energy Density is Also Required, the Above is Limited to Metallized Films

## Slide 3: NanoLamTM - Solid State High Temperature Polymer Capacitors
NanoLamTM capacitors represent a disruptive change in the way in which polymer capacitors are produced
The film extrusion plant, metallizing converter and winding machines are replaced with a single apparatus that is fed with only metal wire and liquid monomer

## Slide 4
Fig. 1. Process of forming a NanoLamTM capacitor using individual capacitor elements that are stacked, connected in parallel and epoxy potted in a polymer box.
Schematic System Used to Produce Solid-State Polymer/Metal Nanolaminate Composite
Typical Nanolaminate Production Machine
One Step NanoLamTM Capacitor Material Manufacturing Process
Aluminum Deposition Station
Mask 1
Mask 2
Bulk Nanolaminate Material

## Slide 5
NanoLamTM Capacitor Manufacturing Process

## Slide 6: High Temperature Polymer Dielectric Materials
The Nanolam Polymer Dielectric is Formed Using Radiation Crosslinked Acrylate Monomers
H2C=CHC(O)O - R(X) - OC(O)CH=CH2
R(X) = Aliphatic, Aromatic, Cycloaliphatic,
Halogen based, etc
Dielectric Constants 2.7<k<9
Dielectric Constant of Current Polymer k=3.2
  Glass Transition Temperature Tg >200oC

## Slide 7
Thickness Range of NanoLamTM Polymers 100nm < t <1000nm
Ultrathin Polymer Dielectrics Have Superior Breakdown Strength
We Found that If a Dielectric Layer has Uniform Thickness and Very Low Surface Roughness
The Breakdown Strength Increases as the Dielectric Thickness Decreases

## Slide 8
Internal Series Sections are Used to Create High Voltage
Capacitor elements (>5000V) Parts
Allows Use of Nanothick Polymer Dielectric with High Breakdown Strength
Oil Vapor Microjets are Used to Form the Series Sections

## Slide 9: Superior Self Healing Properties
The NanoLamTM Polymer is Formulated with high O:C and H:C Ratios in the Chemical Structure
For a Given Electrode Thickness and Applied Voltage, the Efficiency of the Self-Healing Process is Primarily a Function of O:C and H:C Ratios. Carbon and Aluminum From the Breakdown Site are Removed by Conversion Al2O3, CO, CO2, CH3, CH4, and Other Hydrocarbon Gases
Energy Dumped During a Self-healing Event, Is Proportional To V2. Multiple Series Sections Result in Lower Discharge Energy in the Individual Capacitor Zones
Glass Transition Temperature >200oC
No Melting Point

## Slide 10
Self-Healing Property Comparison DC-link Metallized PP Capacitor
and DC-link NanoLamTM Capacitor

## Slide 11
Superior Current Carrying Capacity
Higher Thermal Conductivity Polymer
High Tg >200oC
Capacitor Elements have Lower TCEs than Film Capacitors
Smaller Size Capacitor Elements with More Metal Layers Per Unit volume
Zinc Arc Spray Contacts only Metal Layers (no polymer)

## Slide 12
Performance at Higher Switching Frequencies
Test Range
Test Range
At least Up to 300KHz
L= 21 nH / 1MHz
L= 18 nH / 10MHz
L= 10 nH / 1MHz
L= 6 nH / 10MHz

## Slide 13
Operating
Temp
Operating
Temp
Operating
Temp
Operating
Temp
Variation of Key NanoLamTM Capacitor Properties with Temperature.

## Slide 14
Capacitance Stability as a Function of Temperature

## Slide 15
Stability of Capacitance and ESR of 30µF NanoLamTM Capacitors
as a Function of Temperature at 670VDC.

## Slide 16
Performance of 5µF/670V Capacitor Elements Tested At 1.25xVr/200oC

## Slide 17
Performance of Packaged 30µf NanolamTM Capacitors
Tested At 850V/125oC for 1000hrs and 1250hrs at 670V/160oC.

## Slide 18
NanolamTM 30µf/670V Packaged Capacitors Tested for
Self-healing Event Initiation Voltage.
Vrated

## Slide 19
NanoLamTM 5µF/670V Capacitor Elements Tested for self-healing Event Initiation Voltage at Room Temperature and at -196oC.
Vrated
Vrated

## Slide 20
Summary
Superior Breakdown Strength
The Breakdown Strength of the NanolamTM Dielectric is not Significantly Affected In The Temperature Range Of -196oC To +200oC
Superior Current Performance due to the Unique Dielectric Properties and Capacitor Construction
Temperature Rating with the Current Package: 160oC
In Comparison to High Temperature Films – PEN and PPS
Higher Operating Temperature than PPS with no Derating ( at least +35oC)
>10X Energy density