## Slide 1: High permittivity garnet ferrites for LTCC compatible circulators
LEGAY Mathis
15th October 2026
Noordwijk, Netherlands
Richard LEBOURGEOIS, Rassoul MANSOUR – Thales Research & Technology
Daniel CABAN-CHASTAS, Quentin TODOLI – Thales DMS
Vincent LAUR – Lab-Sticc

## Slide 2: Summary
Context & Objectives
Ferrites synthesis
Design and fabrication of the circulator
Measurements
Conclusion & Perspectives

## Slide 3: Summary
Context & Objectives
Ferrites synthesis
Design and fabrication of the circulator
Measurements
Conclusion & Perspectives

## Slide 4: I. Context & objectives
  Miniaturizing the components and better integration into systems
Application’s field: telecommunication and radar systems
Circulator
T/R module
Bulky
Expensive
Active Electronically Scanned Antennas

## Slide 5: I. Context & objectives
Circulator
  Passive and non-reciprocal component
  Main function: routing microwave signals
    Possibility of simultaneous transmission/reception
    Equipment protection
Phenomenon of signal circulation
3
2
1
TX
RX
2
1
3
HPA
Circulator
Radiating element
Radome
LNA
TX
TX
TX
RX
RX
RX
RX
  Circulator: a crucial element of a T/R module

## Slide 6: I. Context & objectives
Circulator structure
  Ferrite responsible of the circulation phenomenon when submitted to an external magnetic field
  Adding a magnet on the top
Ferrite choice
  Ferrites choice depending on frequency application
L band
S band
C band
X band
Ku band
K band
Ka band
Q band
V band
Garnet
Ms : 300 to 2000 G
Spinel
Ms : 1900 to 5000 G
Hexaferrites
Ms : 3000 to 5000 G
Y-junction using microstrip technology

## Slide 7: I. Context & objectives
Yttrium Iron Garnet - Y3Fe5O12
  Most common garnet
  Properties in line with a X band application
Ms | Permittivity | tan
1800 G | 15 | < 1 x 10-3
Ms | Permittivity | 
1800 G | 15 | < 1 x 10-3
Sintering temperature
1500 °C
BUT
Very high temperature
Objectives of the study
  Modify the properties of the YIG to:
Reduce the size of a circulator
Increase the permittivity of the ferrite
Simplify the manufacturing process
Ferrite compatible with LTCC process

## Slide 8: I. Context & objectives
Angular frequency
Speed of the ligth
R : Radius of the resonnator
: Effective permeability of the ferrite
: Permittivity of the ferrite
Bosma equation1 :
How to reduce the size of circulator?
  Size of a Y-junction resonator gouverned by :
Increase the permittivity of the ferrite
1. H. Bosma, “On Stripline Y-Circulation at UHF,” IEEE TRANSACTIONS ON MICROWAVE THEORY AND TECHNIQUES, p. 12.

## Slide 9: I. Context & objectives
Circulator manufacturing
Magnet
Magnet
  Complex manufacturing
    Multimaterials
    Machining/gluing
    Large size
    Expensive
Assembly
  LTCC : Low Temperature Co-fired Ceramic
    Single step fabrication at 950°C
    No additionnal machining needed
Need to have a « compatible » LTCC ferrite
LTCC process
Green tape
Cutting
Punching of the vias
Filling of the vias
Screenprinting of the connectors
Stacking the alignments
Pressing
Cofiring
Post firing
Electronical adjustment
Simulation
Easier, faster and cheaper than assembling
Reduce the sintering temperature of the ferrite to be able to use the LTCC process

## Slide 10: Summary
Context & Objectives
Ferrites synthesis
Design and fabrication of the circulator
Measurements
Conclusion

## Slide 11: II. Ferrite synthesis
How to manage YIG properties?
  Adjustment of properties via cationic substitutions
Y3Fe5O12
Ca2+
Sn4+
Stabilize saturation magnetization
Y3+
Fe3+
O12
Substitutions
Y2,05Bi0,7Ca0,25Fe4,65Cu0,05Sn0,3O12
Conventional ceramic process
Powder preparation
Powders oxides weighing
Mixing/milling
First heat treatment
Formation of the magnetic phase
Heat treatment
Sintering at high temperature
Densification and completing the phase formation
Bi3+
Cu2+
Decrease of the sintering temperature
Increase in permittivity
Shaping
Uniaxial pressing

## Slide 12: II. Ferrite synthesis
Substituted YIG properties
 | Sintering temperature | ε’ at 9.3GHz | tanδ at 9.3 GHz | Ms (G)
Y3Fe5O12 | 1500°C | 15 | 1.10-3 | 1800
Y2,05Bi0,7Ca0,25Fe4,65Cu0,05Sn0,3O12 |  |  |  | 
Objectives
Decrease of the sintering temperature
Increase of the permittivity
Conservation of low losses
Stabilization of the saturation magnetization
950°C
( )
✓
21
( )
✓
()
3.10-3
✓
1900
( )
✓

## Slide 13: Summary
Context & Objectives
Ferrites synthesis
Design and fabrication of the circulator
Measurements
Conclusion & Perspectives

## Slide 14: III. Design and fabrication of circulator
Contribution of the high permittivity of the ferrite
  Comparison of the dimensions of a circulator with a pure YIG disk with those using a high permittivity substituted garnet
  Y-junction using microstrip technology optimized at 10GHz using ANSYS HFSS and Maxwell 3D
  Ferrite disk of radius R is surrounded by a commercial dielectric with ε’= 20
A 23% decrease in surface area
Pure YIG
ε’=15
tanδ = 1.10-3
ε’=20
tanδ = 1.10-3
Substituted YIG
ε’=21
tanδ = 3.10-3
ε’=20
tanδ = 1.10-3
Design of a circulator with high permittivity ferrite
  Magnetostatic-electromagnetic co-simulations conducted to determine the magnet geometry required to generate a homogeneous field within the ferrite  Samarium-Cobalt magnet

## Slide 15: III. Design and fabrication of circulator
3 Gluing in measurement cell
Before LTCC process : cofiring preliminary test
  Need to check if materials can be cofired
2 Preparation of substrates and deposition of conductive lines
  Substrate Cutting/polishing
  Screen printing deposition of conductive lines
  2 massive pieces formed by uniaxial pressing : Commercial dielectric + ferrite cylinder
  Co-firing at 950°C
1 Pressing/massive cofiring
950°C

## Slide 16: Summary
Context & Objectives
Ferrites synthesis
Design and fabrication of the circulator
Measurements
Conclusion & Perspectives

## Slide 17: IV. Measurements
Measurement setup
  Circulator connected to a Vectorial Network Analyzer
S-parameters
Magnet
Circulator with metallization
Load of 50 Ω
1
2
50 Ω
  , : reflexion losses
  : insertion losses (Goal : the lowest as possible)
  : isolation (Goal : the highest as possible)

## Slide 18: IV. Measurements
5
6
7
8
9
10
11
12
13
14
15
0
- 5
- 10
- 15
- 20
- 25
- 30
- 35
- 40
Frequency (GHz)
dB(S(2,2))
Adaptation
Frequency (GHz)
5
6
7
8
9
10
11
12
13
14
15
0
- 0.1
- 0.2
- 0.3
- 0.4
- 0.5
- 0.6
- 0.7
- 0.8
- 0.9
- 1.0
dB(S(2,1))
Insertion losses
5
6
7
8
9
10
11
12
13
14
15
0
- 5
- 10
- 15
- 20
- 25
- 30
- 35
- 40
Frequency (GHz)
dB(S(1,2))
Isolation
5
6
7
8
9
10
11
12
13
14
15
0
- 5
- 10
- 15
- 20
- 25
- 30
- 35
- 40
Frequency (GHz)
dB(S(1,1))
Adaptation
Simulation
Strong non-reciprocity
Relative bandwith = 48,9% centered at 9,2 GHz
Insertion losses < 0,6 dB with minimum at 0,36dB
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Measurements
Good agreement with simulations
Relative bandwith = 41,6% (slightly shifted to 9,7 GHz for S12)
Insertion losses slightly increased up to 0,6 dB
Reflexion losses
Reflexion losses
Isolation
Insertion losses

## Slide 19: Summary
Context & Objectives
Ferrites synthesis
Design and fabrication of the circulator
Measurements
Conclusion & Perspectives

## Slide 20: V. Conclusion & Perspectives
Synthesis of a substituted YIG with upgraded properties
Fabrication of a demonstrator with this substituted YIG
  Successfully co-fired at 950°C with the commercial dielectric
Good electromagnetic performances (low insertion losses and high isolation)
950°C
( )
Y2,05Bi0,7Ca0,25Fe4,65Cu0,05Sn0,3O12 |  |  |  | 
21
( )
( = )
3.10-3
( = )
1900
  Pave the way for the development of low-cost, compact, and efficient circulators
Perspectives :
  Material development: increase more ferrite permittivity
  Process development: produce a circulator with the complete LTCC process (cofiring all materials including metallic parts)

## Slide 21
Thank you