## Slide 1: Exxelia’s Path to RoHS: Ensuring Reliability in Next-Generation Space capacitors
6TH SPACE PASSIVE COMPONENT DAYS 2026 - ESA/ESTEC
Noordwijk, The Netherlands 13-16 October 2026
Redouane HAMMAL
GBU Capacitors
Exxelia SAS, 105 Rue Géneral Leclerc, 67440, Marmoutier, France
Email : redouane.hammal@exxelia.com

## Slide 2: Exxelia Film Capacitors – PET technology for Space
Exxelia Background in PET Technology
2007
2008
2008 - 2009
2009 - 2012
2013 - 2016
1990
1994
New Series
PM907 - PM948
Miniaturization
Exxelia
Internal Qualif
PM907 - PM948
CNES
ESCC Evaluation
PM907S - PM948S
ESA
Eval & Qualif
PM907S - PM948S
Development of
PM90 - PM94
ESA Eval-Qualif
Continuous Design Improvement for Better Miniaturization & Integration Behavior
2026 - 2027
ESA
New Project
PM907S - PM948S
5 years Testing allowing Proven Reliability Data & Technological Behaviors
The goal of the New Project
Lead Free Transition (RoHS reflow process)
Miniaturization –> Higher Energy Density
Thermal modeling Comsol
Notes: Increase Awareness by innovation (vieilles familles, dernier lancement 1997)
Secure Existing Business (100K€ à risque attaqué par concurrence + 300K€ de legacy business à risque si re-design)
Diversify our Markets (Thruster + Cruise + Indus + Filtering)
Gain Market Share (addresser les marchés où nous ne sommes pas implantés US/Brésil/Corée)
Amortize the New Production Line “MBSAU”

## Slide 3
Project objectives
Objectives:
  Improve temperature capability of SMD metallized PET capacitors for lead-free transition, preserving space-grade lifetime and reliability
  Increase energy density
How to achieve those objectives:
Objectve 1:
  1/ Capacitors:
    Improve the process for better temperature resistance of capacitors
    Simulate the temperature distribution inside the capacitor by Comsol simulation
    Optimize the surface treatment of terminals
  2/ PCB assembly:
    Optimize soldering parameters (temperature cycle)
    Selection of suitable RoHS alloys
    Others: PCB (layer thickness, coating)
Objective 2:
  Scan the full product range and identify capacitance / voltage values where an increase of voltage stress is possible

## Slide 4
Can standard SMD film capacitors be processed as RoHS compliant?
Dielectrics | Technology | Capacitance Range | Voltage Range (VDC) | Re-flow soldering Tmax°C
PET | Wound/Box encapsulated | 0.01µF – 6.8 µF | 63 V – 1000 V | 220° - 250°
PPS |  | 0.01µF – 2.2 µF |  | 250°
PEN | Stacked/Bare | 0.001µF – 4.7 µF | 25 V - 1000 V | 240° - 255°
PPS |  | 1nF – 0.22 µF | 16 V – 50 V | 250° - 260°
PET |  | 10nF – 4.7 uF | 63 V – 630 V | 240° - 245°
Benchmark of commercial SMD film capacitor offerings :
Dielectric films (PET, PEN, PPS).
Technologies (stacked vs. wound) and (Encapsulated vs. Bare)
Commercial offerings mainly focus on lower capacitance ranges.
Our range:
50V to 1250 V
10nF to 200µF
Stacked vs.wound

## Slide 5
Which dielectric is the best candidate ?
Property | PP (Standard) | PPHT | PET (Standard) | PEN | PPS
Relative Permittivity | 2,2 | 2,2 | 3,2 | 3 | 3
Breakdown | 600 V/µm | 700 V/µm | 350 V/µm | 300 V/µm | 350 V/µm
Operating voltage stress | 200-250 V/µm | 200-250 V/µm | 125 V/µm | 100 V/µm | 80 V/µm
Melting point Temperature | 168°C | 173°C | 255°C | 265°C | 285°C
Max operating Temperature | 105°C | 140°C | 125°C | 150°C | 180°C
Self-Healing | Excellent | Excellent | Good | Moderate | Poor
Min, Thickness (µm) | 2,2 | 1,9 | 0,9 | 1,4 | 1,2
Dissipation Factor (ESR) | Very Low | Very Low | High | Moderate | Low
Conclusion | (-) : Melting point too low for reflow. Low permittivity prevents miniaturization. REJECTED | (-) : Melting point too low for reflow. Low permittivity prevents miniaturization. REJECTED | (-) : Melting point and Max temperature low for lead-free reflow. CANDIDATE | (-) : Limits high-gradient designs. CANDIDATE | (-) Poor self-healing; limits miniaturization. REJECTED
PET and PEN => best candidates
Selection based on the optimal compromise between temperature resistance and dielectric thickness.

## Slide 6
Example of non RoHS reflow profile
Reflow Soldering Optimization
Adapting standard reflow recommendations to high-reliability space constraints.
Process Control (3 Phases):
  Pre-heating: Safe temperature rise to avoid thermal stress.
  Soldering: Optimized peak Tmax and time to protect the component.
  Cooling: Gradual cool-down to prevent micro-cracks.
Reliability: Temperature tracking (no overshoot) and optimized internal heat treatments.
Challenges for RoHS
compliant process:
RoHS solder allows need higher temperature
Heat should not damage the dielectric

## Slide 7
Critical technical challenges
Thermal Gap (+30°C):
Reflow peak reaches 245°C–250°C, inducing severe thermal stress on the metallized PET dielectric film.
IMC Growth:
Accelerated Intermetallic Compound formation at higher lead-free temperatures, impacting joint integrity.
Process window narrowing:
Balancing optimal wetting with voiding control to prevent mechanical failure under launch vibrations.
Critical Technical Challenges

## Slide 8
Simulation

## Slide 9
Simulation

## Slide 10
Scope of the work
Scope of the work
  Exxelia PM series (PET dielectric for space applications).
  SMD variants suitable for reflow soldering.
Group 3: Miniaturization (Higher Voltage)
Voltage step-stress | temp step-stress Temp cycling | endurance
Group 2: Validation of Settings
Temp cycling | vibration testing Step-stress | endurance
Group 1: PCB Soldering Cycle
Solder parameters definition
Thermal cycling, step-stress & endurance
Reference | Capacitance (µF) | Voltage(Vdc)
Ref1 0.82µF 400V | 0.82 | 400
Ref3 10µF 250V | 10 | 250
Ref2 15µF 63V | 15 | 63
Ref4 1,2µF 630V | 1,2 | 630
Ref4 10µF 50V | 10 | 50
Ref4 12µF 170V | 12 | 170
Test vehicles to be manufactured

## Slide 11
Miniaturization
Rated voltage (Vdc) | Optimized voltage stress | Possibility to increase voltage stress
63 | No | No thinner gauge
100 / 170 | Almost | Too high stress with thinner gauge
250 | No | Too high stress with thinner gauge
from 400 V to 1250 V | No | Yes
Reference | Capacitance (µF) | Voltage (Vdc) | Current dimension (mm) | New dimension (mm) | Energy density increase (%)
PM907 | 3.9 | 630 | 31x22x32 | 31x12.5x32 | 40%
PM948S | 1,2 | 630 | 18.5x17x17 | 18.5x15x17 | 12%
Expected energy density increase: between +10 and +40%

## Slide 12
Evaluation tests and analysis
Solder quality check by DPA

## Slide 13: Thank you for your attention Questions & Answers
Redouane HAMMAL
GBU Capacitors
Exxelia SAS, 105 Rue Géneral Leclerc, 67440, Marmoutier, France
Email : redouane.hammal@exxelia.com

## Slide 14
Advantages of PET Technology
Better Power Behaviors
Even Lower Energy Density
CPET ~ 60-70% CX7R
Example of Comparison