## Slide 1
MINCOR - Minimisation of crystal oscillator cosmic radiation effects
Follow up & conclusion
Nicolas GUFFLET, Laurent COUTELEAU, Rami KHOURI / RAKON
Yannick PADIE, Alexandre ROUSSET / TRAD
ESA contract No. 4000133592/20/NL/FE
6th SPACE PASSIVE COMPONENT DAYS - SPCD 2026
13-16 October 2026 | ESA/ESTEC
Noordwijk, The Netherland

## Slide 2
Reminder
Presentation of results
Conclusion and perspective
Table of content

## Slide 3
Resonator : passive component
Oscillator : active component
Main word : frequency F ~ 5…150MHz and especially frequency stability : DF/ F : 10-6 … 10-10 … 10-14
Designed to be insensitive to external environnement : temperature, acceleration, pressure, time,… and radiation
Reminder : Quartz resonator & oscillator

## Slide 4
Radiation may generate frequency drift at low dose rate (LDR) and cumulated over the mission duration (TID)
Radiation profiles depend on mission and LDR will have a special role in LEO where there is periodic radiation cycles
Radiation sensitivity
Dose rate mapping for Telecom LEO orbit. 3D view (left) ; Planisphere view (right)

## Slide 5
Sensitivity to cycling LDR is assessed before and after a 100krad deposition
Test plan realized
High dose 100krad
deposition
on resonator
Device characterization
Device characterization
Device characterization
Device characterization
Low dose rate Cycling
Few rad/h
Radiation ON / OFF cycling with continuous measurement of frequency in dummy oscillator
Continuous frequency measurement
Frequency measurement before/after
Low dose rate Cycling
Few rad/h
Radiation ON / OFF cycling with continuous measurement of frequency in dummy oscillator
Continuous frequency measurement

## Slide 6
Use of a Cobalt 60 gamma ray source at few rad/h
Resonator measurement in dummy oscillator
Radiation ON/OFF cycle done with a moveable lead wall (*)
LDR cycling sensitivity assessment
Oscillator structured so as to expose ony the resonator in the beam
Test oscillators
Motorized shield open
Image of the lead wall from the source
Measurement system
*Note: lead wall not fully opaque to gamma ray : 10% transparency

## Slide 7
Use of Cobalt 60 gamma ray source
100krad deposited @ 220rad/h during roughly 20 days
Done on resonator only to avoid the effect of the oscillator
High dose deposition
Board with 60 resonators for 100krad TID

## Slide 8
15 variants with different design and processes (frequency enclosure, cut, material, electrodes,…)
6 variants for T1507 10MHz SC-cut resonators
8 variants for T807 100MHz AT- and SC-cut resonators
1 variant for SMD 50MHz AT-cut resonators
200+ resonators produced over the 15 groups with all corresponding datapackages
Resonators produced as per specification on the ESCC3501 qualified line
In each group, 4 pieces selected as considered to be representative
60 resonators in total available for radiation tests
Test vehicules used

## Slide 9
Cumulative positive frequency drift
Osc. 10MHz n°1
Basic behaviours under LDR cycling
Frequency variation overview (left) and slopes comparison (right) for Osc. 10MHz n°1
In this example, values of 2.6.10-11/rad can be deduced
2 differents cycles applied @ 6 rad/h
Cycle 1 : 20min ON / 100min OFF
Cycle 2 : 120min ON / 120min OFF

## Slide 10
Linear slopes with clear transition at ON/OFF period
Osc. 10MHz n°1
Basic behaviours under LDR cycling
Frequency variation during irradiation cycling 1 (left) and 2 (right) for Osc. 10MHz n°1

## Slide 11
Slopes are correlating also when looked within each ON or OFF period
Osc. 10MHz n°1
Basic behaviours under LDR cycling
Frequency variation during ON/OFF periods for cycle 1 (left) and cycle 2 (right) for Osc. 10MHz n°1

## Slide 12
Cumulative positive frequency drift superimposed with sudden but reversible positive frequency drift
Osc. 10MHz n°2
Other signatures
Frequency variation during stabilization and irradiation cycling for Osc. 10MHz n°2
Sudden positive frequency shift around 2.5e-11 in this example
with relaxation-like behavior when coming back

## Slide 13
Cumulative positive frequency drift superimposed with sudden but reversible negative frequency drift
Osc. 10MHz n°11
Other signatures
Frequency variation during stabilization and irradiation cycling for Osc. 10MHz n°11
Relaxation-like behavior at beginning of OFF period leads to quite jagged curves

## Slide 14
Non cumulative positive frequency drift with a kind of saturation effect
Osc. 10MHz n°5
Other signatures
Frequency variation during stabilization and irradiation cycling for Osc. 10MHz n° 5 (swept material)

## Slide 15
At this level, the phenomena are not linear hence equilibrium depends upon ON/OFF cycle durations
Osc. 10MHz n°5
Equilibrium depends on duration
Frequency variation during ON/OFF periods for cycle 1 (left) and cycle 2 (right) for Osc. 10MHz n° 5
Slope around 1.75.10-11/rad
Slope around 0.85.10-11/rad

## Slide 16
Time to stabilize linked to the resonator sensitivity shows impact of wall transparency
Effect of the lead wall transparency
…
Frequency drift correlation between pre-cycling (B) and cycling 2 (D)

## Slide 17
Resonators produced in the study do not present LDR sensitivity at these frequencies
To be noticed that 50MHz where produced using non swept Standard Quality quartz
Osc. 100MHz n°4 and Osc. 50MHz n°4
Signatures of the 50 and 100MHz
Frequency variation during ON/OFF periods for Osc. 100MHz n°4 (left) and Osc. 50MHz n°4 (right)

## Slide 18
Change of frequency before/after TID : Frequency variations before and after the 100krad TID remain below few 10-12/rad for all 60 resonators
LDR sensitivity after TID : stabilize and possibly reverse
After 100krad TID
LDR sensitivity after TID for Osc. 10MHz n°1 (left) and Osc. 100MHz n°2 (right)
Negative slope during radiation

## Slide 19
In this presentation we exposed some results of the MINCOR project :
  Different kind of signature during LDR cycling (cumulative/non-cumulative, fast/slow, positive/negative…)
  Order of magnitude in the range of few 10-11/rad in LDR cycling
  10MHz resonators present a signature
  50MHz and 100MHz do not present LDR sensitivity at the measurable level
  Relative frequency changes of few 10-12/rad over 100krad (non-linear effect)
  Saturation effect clearly visible on swept material without pre-irradiation
  Saturation effect clearly visible with pre-irradiation on non swept material
  Radiation sensitivity could not be linked to other process parameters
Synthesis

## Slide 20
What does it imply for LEO ?
For LEO particularly, it is important to take the LDR cycling into account not only the TID
The sensitivity to radiation must be seen as per the need :
  zero does not exist. Pass/Fail criteria depends on the specification, on design and on mission profile (path and duration)
  In a lot of application values of few 10-11/rad will be fully sufficient
  In more demanding LEO applications, swept material is recommended because already stabilized
  If needed a pre irradiation can be performed
  This must be decided at manufacturer level : know your products !
W.r.t. quartz material : Low impurities content is needed however the main challenge is to have values guaranteed by suppliers.
In the present study the worse material had impurities measured @ 1ppm which remains low but could not be guaranteed by supplier.
Perspective

## Slide 21
Thank you !
www.rakon.com
Equipment • Subsystems • Oscillators • Filters • Resonators